KEY TEST DATA SUMMARY FOR THE MONTH OF FEBRUARY,  2024/2025           Page  1
     ________________________________________________________________________________ _____________
     |              |                                        |       |              |              |
     |              |               PRESALE DATA             |       |STAPLE  DATA  |COLOUR  DATA  |
     |              |  LOTS    BALES     B/L  |BALE WT   WT  | RAPID | LOTS    AR%  | LOTS    AR%  |
     |______________|_________________________|______________|_______|______________|______________|
     | 2023/2024:   |                         |              |       |              |              |
     |   Queensland |    141       644   4.57 | 178.4        |  5.0  |    96  63.0  |     0   0.0  |
     |   NSW        |   8621     42543   4.93 | 176.1        | 32.8  |  4735  58.4  |     0   0.0  |
     |   Victoria   |  11004     65644   5.97 | 177.4        | 40.1  |  5870  51.1  |     0   0.0  |
     |   Tasmania   |    444      2688   6.05 | 172.9        | 16.4  |   235  49.3  |     0   0.0  |
     |   SA         |   3128     17816   5.70 | 179.8        | 44.2  |  2015  66.7  |     0   0.0  |
     |   WA         |   5493     39401   7.17 | 178.0        | 87.8  |  4072  79.0  |     0   0.0  |
     |--------------|-------------------------|--------------|-------|--------------|--------------|
     |   Australia  |  28831    168736   5.85 | 177.4        | 46.9  | 17023  61.1  |     0   0.0  |
     |--------------|-------------------------|--------------|-------|--------------|--------------|
     | TYPE:        |                         |              |       |              |              |
     |   Fleece     |  16327    107972   6.61 | 179.2        | 46.4  | 12571  74.8  |     0   0.0  |
     |   Skirting   |   6396     29996   4.69 | 175.5        | 46.6  |  3449  55.5  |     0   0.0  |
     |   Carding    |   6108     30768   5.04 | 172.6        | 48.8  |  1003  18.5  |     0   0.0  |
     |==============|=========================|==============|=======|==============|==============|
     | 2024/2025:   |                         |              |       |              |              |
     |   Queensland |    137       707   5.16 | 182.3        |  8.0  |    97  79.6  |     0   0.0  |
     |   NSW        |   8133     42826   5.27 | 176.5        | 22.7  |  4617  60.5  |     0   0.0  |
     |   Victoria   |  10321     63079   6.11 | 176.7        | 25.9  |  5392  50.6  |     0   0.0  |
     |   Tasmania   |    488      2983   6.11 | 175.8        |  9.8  |   256  46.8  |     0   0.0  |
     |   SA         |   1854     10229   5.52 | 177.2        | 37.6  |  1155  64.9  |     0   0.0  |
     |   WA         |   4781     33094   6.92 | 178.6        | 83.6  |  3612  80.9  |     0   0.0  |
     |--------------|-------------------------|--------------|-------|--------------|--------------|
     |   Australia  |  25714    152918   5.95 | 177.1        | 36.0  | 15129  60.9  |     0   0.0  |
     |--------------|-------------------------|--------------|-------|--------------|--------------|
     | TYPE:        |                         |              |       |              |              |
     |   Fleece     |  14503     98121   6.77 | 179.1        | 35.9  | 11183  74.5  |     0   0.0  |
     |   Skirting   |   5737     27399   4.78 | 175.6        | 34.9  |  3134  57.3  |     0   0.0  |
     |   Carding    |   5474     27398   5.01 | 171.4        | 37.7  |   812  15.8  |     0   0.0  |
     |==============|=========================|==============|=======|==============|==============|
     | DIFFERENCES: |                         |              |       |              |              |
     |   Queensland |    2.8-     9.8    0.59 |  2.2   12.2  |  3.0  |  1.0   16.6  |  0.0    0.0  |
     |   NSW        |    5.7-     0.7    0.34 |  0.2    0.9  | 10.1- |  2.5-   2.1  |  0.0    0.0  |
     |   Victoria   |    6.2-     3.9-   0.14 |  0.4-   4.3- | 14.2- |  8.1-   0.5- |  0.0    0.0  |
     |   Tasmania   |    9.9     11.0    0.06 |  1.7   12.8  |  6.6- |  8.9    2.5- |  0.0    0.0  |
     |   SA         |   40.7-    42.6-   0.18-|  1.4-  43.4- |  6.6- | 42.7-   1.8- |  0.0    0.0  |
     |   WA         |   13.0-    16.0-   0.25-|  0.3   15.7- |  4.2- | 11.3-   1.9  |  0.0    0.0  |
     |--------------|-------------------------|--------------|-------|--------------|--------------|
     |   Australia  |   10.8-     9.4-   0.10 |  0.2-   9.5- | 10.9- | 11.1-   0.2- |  0.0    0.0  |
     |--------------|-------------------------|--------------|-------|--------------|--------------|
     |   Fleece     |   11.2-     9.1-   0.16 |  0.1-   9.2- | 10.5- | 11.0-   0.3- |  0.0    0.0  |
     |   Skirting   |   10.3-     8.7-   0.09 |  0.1    8.6- | 11.7- |  9.1-   1.8  |  0.0    0.0  |
     |   Carding    |   10.4-    11.0-   0.03-|  0.7-  11.5- | 11.1- | 19.0-   2.7- |  0.0    0.0  |
     |______________|_________________________|______________|______________________|______________|

     NOTE: Differences for LOTS, BALES, AV BALE WT, WT, PROJECTED WT, L&S and COLOUR are % differences.
           Differences for LOT-SIZE (B/L), RAPID% and AR% are actual values.
           Adoption Rate (AR%) data is based on number of bales tested as a % of number of bales tested for YIELD.
           Adoption Rate (AR%) for STAPLE and COLOUR Data is based on all wool tested.

                           KEY TEST DATA SUMMARY - JULY TO FEBRUARY,  2024/2025                      Page  2
      _____________________________________________________________________________________________________
     |              |                                        |       |       |              |              |
     |              |               PRESALE DATA             |       |       |STAPLE  DATA  |COLOUR   DATA |
     |              |  LOTS     BALES     B/L |BALE WT  WT   |PROJ WT| RAPID | LOTS    AR%  | LOTS     AR% |
     |______________|_________________________|______________|_______|_______|______________|______________|
     | 2023/2024:   |                         |              |       |       |              |              |
     |   Queensland |   4654     29734   6.39 | 182.3        |       | 10.6  |  3445   79.2 |     0    0.0 |
     |   NSW        |  71790    361298   5.03 | 176.9        |       | 29.3  | 43562   64.2 |     0    0.0 |
     |   Victoria   |  78675    452348   5.75 | 178.6        |       | 40.8  | 45796   57.2 |     3    0.0 |
     |   Tasmania   |   4565     25167   5.51 | 177.2        |       |  8.8  |  2974   61.8 |     0    0.0 |
     |   SA         |  24867    144349   5.80 | 180.8        |       | 34.9  | 16239   69.0 |     0    0.0 |
     |   WA         |  34167    235755   6.90 | 178.1        |       | 85.6  | 24560   76.1 |     0    0.0 |
     |--------------|-------------------------|--------------|-------|-------|--------------|--------------|
     |   Australia  | 218718   1248651   5.71 | 178.3        |       | 42.0  |136576   64.8 |     3    0.0 |
     |--------------|-------------------------|--------------|-------|-------|--------------|--------------|
     | TYPE:        |                         |              |       |       |              |              |
     |   Fleece     | 127676    815955   6.39 | 179.9        |       | 41.1  |103160   78.8 |     3    0.0 |
     |   Skirting   |  51674    242255   4.69 | 175.9        |       | 41.5  | 28295   57.0 |     0    0.0 |
     |   Carding    |  39368    190441   4.84 | 174.6        |       | 45.8  |  5121   14.6 |     0    0.0 |
     |==============|=========================|==============|=======|=======|==============|==============|
     | 2024/2025:   |                         |              |       |       |              |              |
     |   Queensland |   2825     17426   6.17 | 183.8        |       |  2.9  |  2142   82.1 |     0    0.0 |
     |   NSW        |  66101    341239   5.16 | 177.9        |       | 25.9  | 40168   65.0 |     0    0.0 |
     |   Victoria   |  75140    458234   6.10 | 178.9        |       | 27.9  | 45026   59.3 |     0    0.0 |
     |   Tasmania   |   5373     29656   5.52 | 177.1        |       | 25.5  |  3676   65.0 |     0    0.0 |
     |   SA         |  14819     84839   5.73 | 180.2        |       | 29.4  |  9524   67.4 |     0    0.0 |
     |   WA         |  28858    191583   6.64 | 178.4        |       | 84.4  | 21100   77.2 |     0    0.0 |
     |--------------|-------------------------|--------------|-------|-------|--------------|--------------|
     |   Australia  | 193116   1122977   5.82 | 178.7        |       | 35.3  |121636   65.2 |     0    0.0 |
     |--------------|-------------------------|--------------|-------|-------|--------------|--------------|
     | TYPE:        |                         |              |       |       |              |              |
     |   Fleece     | 114099    740936   6.49 | 180.3        |       | 34.1  | 92513   79.0 |     0    0.0 |
     |   Skirting   |  44904    214868   4.79 | 176.6        |       | 35.7  | 24806   57.5 |     0    0.0 |
     |   Carding    |  34113    167173   4.90 | 173.9        |       | 38.8  |  4317   13.8 |     0    0.0 |
     |==============|=========================|==============|=======|=======|==============|==============|
     | DIFFERENCES: |                         |              |       |       |              |              |
     |   Queensland |   39.3-    41.4-   0.22-|   0.8   40.9-|  38.3-|  7.7- |  37.8-   2.9 |  0.0     0.0 |
     |   NSW        |    7.9-     5.6-   0.13 |   0.6    5.0-|   3.2-|  3.4- |   7.8-   0.8 |  0.0     0.0 |
     |   Victoria   |    4.5-     1.3    0.35 |   0.2    1.5 |   3.1 | 12.9- |   1.7-   2.1 |100.0-    0.0 |
     |   Tasmania   |   17.7     17.8    0.01 |   0.1-  17.8 |  16.0 | 16.7  |  23.6    3.2 |  0.0     0.0 |
     |   SA         |   40.4-    41.2-   0.07-|   0.3-  41.4-|  37.6-|  5.5- |  41.4-   1.6-|  0.0     0.0 |
     |   WA         |   15.5-    18.7-   0.26-|   0.2   18.6-|  15.9-|  1.2- |  14.1-   1.1 |  0.0     0.0 |
     |--------------|-------------------------|--------------|-------|-------|--------------|--------------|
     |   Australia  |   11.7-    10.1-   0.11 |   0.2    9.9-|   7.5-|  6.7- |  10.9-   0.4 |100.0-    0.0 |
     |--------------|-------------------------|--------------|-------|-------|--------------|--------------|
     |   Fleece     |   10.6-     9.2-   0.10 |   0.2    9.0-|       |  7.0- |  10.3-   0.2 |100.0-    0.0 |
     |   Skirting   |   13.1-    11.3-   0.10 |   0.4   11.0-|       |  5.8- |  12.3-   0.5 |  0.0     0.0 |
     |   Carding    |   13.3-    12.2-   0.06 |   0.4-  12.6-|       |  7.0- |  15.7-   0.8-|  0.0     0.0 |
     |______________|_________________________|______________|_______|_______|______________|______________|

     NOTE: Differences for LOTS, BALES, AV BALE WT, WT, PROJECTED WT, L&S and COLOUR are % differences.
           Differences for LOT-SIZE (B/L), RAPID% and AR% are actual values.
           The change in PROJECTED WT of wool tested = the % change in WT, adjusted for differences in the WT
           tested at the end of FEBRUARY  as a % of the 12 months total, over the last 3 years.
           Adoption Rate (AR%) data is based on number of bales tested as a % of number of bales tested for YIELD.
           Adoption Rate (AR%) for STAPLE and COLOUR data is based on all wool tested.
           Change in SUPERFINE production (ktonnes) = -3.9%.
           It has moved from 53.8% of the clip at the end of FEBRUARY last year to 57.3% this year.

                         KEY TEST DATA SUMMARY FOR THE MONTH OF FEBRUARY,  2024/2025                      Page  3
      __________________________________________________________________________________________________________
     |              |                                                                                           |
     |              |                                       TEST RESULTS                                        |
     |              |YIELD   VM    MFD    CVD   |  SL    CVSL    SS   CVSS   MIDBRK TIPBRK  HAUT  |  Y     Y-Z  |
     |______________|___________________________|_________________________________________________|_____________|
     | 2023/2024:   |                           |                                                 |             |
     |   Queensland | 62.7   3.5   20.4   21.5  | 78.1   15.8   36.8   33.5   53.5   15.2   64.8  |  0.0   0.0  |
     |   NSW        | 66.1   2.4   21.0   21.2  | 83.5   16.0   35.7   32.6   50.3   21.3   67.3  |  0.0   0.0  |
     |   Victoria   | 68.0   1.5   22.8   21.7  | 86.0   15.6   36.8   33.3   47.0   32.9   71.8  |  0.0   0.0  |
     |   Tasmania   | 71.1   0.7   22.0   22.5  | 86.3   17.1   35.5   33.5   50.7   18.4   68.8  |  0.0   0.0  |
     |   SA         | 62.3   2.6   20.7   21.3  | 88.9   15.5   34.7   35.4   47.8   29.7   71.9  |  0.0   0.0  |
     |   WA         | 61.9   1.9   19.1   20.6  | 86.0   16.5   28.8   39.5   45.3   28.1   67.5  |  0.0   0.0  |
     |--------------|---------------------------|-------------------------------------------------|-------------|
     |   Australia  | 65.5   1.9   21.2   21.3  | 85.7   16.0   33.9   35.2   47.4   28.0   69.4  |  0.0   0.0  |
     |--------------|---------------------------|-------------------------------------------------|-------------|
     | TYPE:        |                           |                                                 |             |
     |   Fleece     | 68.5   1.2   21.5   20.5  | 88.9   15.0   35.2   35.2   48.2   28.8   73.0  |  0.0   0.0  |
     |   Skirting   | 55.9   4.2   19.7   21.8  | 78.2   20.6   28.3   40.7   52.2   21.2   58.8  |  0.0   0.0  |
     |   Carding    | 64.0   2.2   21.9   23.8  | 60.7   17.4   31.1   19.0   21.8   37.5   46.6  |  0.0   0.0  |
     |==============|===========================|=================================================|=============|
     | 2024/2025:   |                           |                                                 |             |
     |   Queensland | 63.8   3.4   18.5   20.0  | 84.3   16.4   34.9   34.7   52.9   10.0   67.4  |  0.0   0.0  |
     |   NSW        | 65.4   2.9   21.0   21.0  | 85.0   15.7   33.9   33.8   49.9   21.6   68.0  |  0.0   0.0  |
     |   Victoria   | 65.0   1.9   22.2   22.4  | 85.5   15.3   31.7   37.0   52.6   26.5   67.9  |  0.0   0.0  |
     |   Tasmania   | 70.2   0.8   22.2   22.6  | 89.7   16.1   34.1   34.1   53.4   23.7   71.2  |  0.0   0.0  |
     |   SA         | 59.8   2.8   20.5   22.0  | 87.0   15.5   30.0   38.7   51.0   24.5   67.5  |  0.0   0.0  |
     |   WA         | 61.7   2.1   18.9   21.0  | 85.1   16.4   27.7   40.2   46.2   34.7   66.6  |  0.0   0.0  |
     |--------------|---------------------------|-------------------------------------------------|-------------|
     |   Australia  | 64.1   2.3   21.0   21.7  | 85.4   15.8   31.1   37.1   49.9   27.2   67.6  |  0.0   0.0  |
     |--------------|---------------------------|-------------------------------------------------|-------------|
     | TYPE:        |                           |                                                 |             |
     |   Fleece     | 67.1   1.4   21.2   20.9  | 88.3   14.8   32.2   37.1   50.8   27.8   70.9  |  0.0   0.0  |
     |   Skirting   | 54.6   5.0   19.3   22.0  | 78.0   20.3   26.2   41.7   53.6   20.8   57.3  |  0.0   0.0  |
     |   Carding    | 63.0   2.5   22.0   24.2  | 60.6   16.7   29.7   20.4   20.5   40.7   46.6  |  0.0   0.0  |
     |==============|===========================|=================================================|=============|
     | DIFFERENCES: |                           |                                                 |             |
     |   Queensland |  1.1   0.1-   1.9-   1.5- |  6.2    0.6    1.9-   1.2    0.6-   5.2-   2.6  |  0.0   0.0  |
     |   NSW        |  0.7-  0.5    0.0    0.2- |  1.5    0.3-   1.8-   1.2    0.4-   0.3    0.7  |  0.0   0.0  |
     |   Victoria   |  3.0-  0.4    0.6-   0.7  |  0.5-   0.3-   5.1-   3.7    5.6    6.4-   3.9- |  0.0   0.0  |
     |   Tasmania   |  0.9-  0.1    0.2    0.1  |  3.4    1.0-   1.4-   0.6    2.7    5.3    2.4  |  0.0   0.0  |
     |   SA         |  2.5-  0.2    0.2-   0.7  |  1.9-   0.0    4.7-   3.3    3.2    5.2-   4.4- |  0.0   0.0  |
     |   WA         |  0.2-  0.2    0.2-   0.4  |  0.9-   0.1-   1.1-   0.7    0.9    6.6    0.9- |  0.0   0.0  |
     |--------------|---------------------------|-------------------------------------------------|-------------|
     |   Australia  |  1.4-  0.4    0.2-   0.4  |  0.3-   0.2-   2.8-   1.9    2.5    0.8-   1.8- |  0.0   0.0  |
     |--------------|---------------------------|-------------------------------------------------|-------------|
     |   Fleece     |  1.4-  0.2    0.3-   0.4  |  0.6-   0.2-   3.0-   1.9    2.6    1.0-   2.1- |  0.0   0.0  |
     |   Skirting   |  1.3-  0.8    0.4-   0.2  |  0.2-   0.3-   2.1-   1.0    1.4    0.4-   1.5- |  0.0   0.0  |
     |   Carding    |  1.0-  0.3    0.1    0.4  |  0.1-   0.7-   1.4-   1.4    1.3-   3.2    0.0  |  0.0   0.0  |
     |______________|___________________________|_________________________________________________|_____________|

     NOTE: Hauteur is calculated using the TEAM-3 formulae as of July 1st, 2006.

                               KEY TEST DATA SUMMARY - JULY TO FEBRUARY,  2024/2025                       Page  4
      __________________________________________________________________________________________________________
     |              |                                                                                           |
     |              |                                       TEST RESULTS                                        |
     |              |YIELD   VM    MFD    CVD   |  SL    CVSL    SS   CVSS   MIDBRK TIPBRK  HAUT  |  Y     Y-Z  |
     |______________|___________________________|_________________________________________________|_____________|
     | 2023/2024:   |                           |                                                 |             |
     |   Queensland | 63.6   4.5   19.6   20.1  | 87.3   15.8   39.2   33.0   48.5   14.8   72.4  |  0.0   0.0  |
     |   NSW        | 67.3   2.6   20.6   20.8  | 85.1   15.9   37.4   32.2   50.1   19.9   69.4  |  0.0   0.0  |
     |   Victoria   | 66.9   2.0   21.9   21.5  | 88.9   15.5   35.8   34.4   50.8   22.8   71.9  | 74.1   7.7  |
     |   Tasmania   | 71.1   0.9   20.7   21.5  | 86.9   16.0   37.7   32.0   44.1   19.3   71.8  |  0.0   0.0  |
     |   SA         | 62.7   3.0   20.6   21.3  | 91.3   15.5   34.3   36.6   51.1   20.3   72.5  |  0.0   0.0  |
     |   WA         | 63.5   1.7   19.1   21.0  | 87.8   16.6   29.7   39.3   49.2   20.8   68.6  |  0.0   0.0  |
     |--------------|---------------------------|-------------------------------------------------|-------------|
     |   Australia  | 65.9   2.3   20.8   21.2  | 87.8   15.9   34.9   35.0   50.1   20.9   70.6  | 74.1   7.7  |
     |--------------|---------------------------|-------------------------------------------------|-------------|
     | TYPE:        |                           |                                                 |             |
     |   Fleece     | 69.6   1.4   21.1   20.4  | 90.5   14.9   36.2   34.7   50.7   20.6   73.8  | 74.1   7.7  |
     |   Skirting   | 56.3   5.0   19.5   21.8  | 80.7   20.4   29.7   39.9   53.3   19.4   60.5  |  0.0   0.0  |
     |   Carding    | 62.0   2.8   21.1   23.7  | 60.3   17.1   29.2   18.2   21.2   35.6   43.7  |  0.0   0.0  |
     |==============|===========================|=================================================|=============|
     | 2024/2025:   |                           |                                                 |             |
     |   Queensland | 63.4   3.4   19.1   20.2  | 89.0   15.1   35.8   33.4   48.0   35.3   72.7  |  0.0   0.0  |
     |   NSW        | 66.7   2.6   20.5   20.8  | 87.5   15.5   36.3   32.6   45.3   26.0   71.1  |  0.0   0.0  |
     |   Victoria   | 65.1   2.0   21.4   21.9  | 89.5   15.4   34.5   36.1   46.1   18.6   72.2  |  0.0   0.0  |
     |   Tasmania   | 70.5   0.7   20.2   21.5  | 89.2   15.8   35.9   32.9   42.1   21.6   72.4  |  0.0   0.0  |
     |   SA         | 60.7   2.9   20.4   21.8  | 89.8   15.6   32.8   38.6   45.3   17.4   71.5  |  0.0   0.0  |
     |   WA         | 62.9   1.7   18.8   21.4  | 86.6   16.5   28.0   40.5   48.5   20.6   67.0  |  0.0   0.0  |
     |--------------|---------------------------|-------------------------------------------------|-------------|
     |   Australia  | 65.0   2.2   20.5   21.4  | 88.3   15.7   33.7   36.0   46.2   21.6   70.8  |  0.0   0.0  |
     |--------------|---------------------------|-------------------------------------------------|-------------|
     | TYPE:        |                           |                                                 |             |
     |   Fleece     | 68.5   1.4   20.7   20.7  | 90.9   14.7   34.9   35.7   46.4   21.4   74.0  |  0.0   0.0  |
     |   Skirting   | 55.2   4.9   19.2   21.9  | 80.8   20.0   29.2   40.4   50.7   19.8   60.9  |  0.0   0.0  |
     |   Carding    | 61.6   2.6   21.2   24.1  | 59.7   17.0   26.3   18.1   18.1   37.0   41.3  |  0.0   0.0  |
     |==============|===========================|=================================================|=============|
     | DIFFERENCES: |                           |                                                 |             |
     |   Queensland |  0.2-  1.1-   0.5-   0.1  |  1.7    0.7-   3.4-   0.4    0.5-  20.5    0.3  |  0.0   0.0  |
     |   NSW        |  0.6-  0.0    0.1-   0.0  |  2.4    0.4-   1.1-   0.4    4.8-   6.1    1.7  |  0.0   0.0  |
     |   Victoria   |  1.8-  0.0    0.5-   0.4  |  0.6    0.1-   1.3-   1.7    4.7-   4.2-   0.3  | 74.1-  7.7- |
     |   Tasmania   |  0.6-  0.2-   0.5-   0.0  |  2.3    0.2-   1.8-   0.9    2.0-   2.3    0.6  |  0.0   0.0  |
     |   SA         |  2.0-  0.1-   0.2-   0.5  |  1.5-   0.1    1.5-   2.0    5.8-   2.9-   1.0- |  0.0   0.0  |
     |   WA         |  0.6-  0.0    0.3-   0.4  |  1.2-   0.1-   1.7-   1.2    0.7-   0.2-   1.6- |  0.0   0.0  |
     |--------------|---------------------------|-------------------------------------------------|-------------|
     |   Australia  |  0.9-  0.1-   0.3-   0.2  |  0.5    0.2-   1.2-   1.0    3.9-   0.7    0.2  | 74.1-  7.7- |
     |--------------|---------------------------|-------------------------------------------------|-------------|
     |   Fleece     |  1.1-  0.0    0.4-   0.3  |  0.4    0.2-   1.3-   1.0    4.3-   0.8    0.2  | 74.1-  7.7- |
     |   Skirting   |  1.1-  0.1-   0.3-   0.1  |  0.1    0.4-   0.5-   0.5    2.6-   0.4    0.4  |  0.0   0.0  |
     |   Carding    |  0.4-  0.2-   0.1    0.4  |  0.6-   0.1-   2.9-   0.1-   3.1-   1.4    2.4- |  0.0   0.0  |
     |______________|___________________________|_________________________________________________|_____________|

     NOTE: Hauteur is calculated using the TEAM-3 formulae as of July 1st, 2006.

                            AWTA Ltd KEY TEST DATA SUMMARY - JULY TO FEBRUARY,  2024/2025                                 Page  5
      __________________________________________________________________________________________________________________________
     |              |                          |             |             |                                                    |
     |              |        PRESALE DATA      |STAPLE  DATA |COLOUR  DATA |                    TEST RESULTS                    |
     |              | LOTS      BALES    WEIGHT| LOTS   AR%  | LOTS    AR% |YIELD  VM  MFD   CVD  | SL    SS  MIDBRK HAUT |YELL |
     |______________|__________________________|_____________|_____________|______________________|_______________________|_____|
     | 2023/2024:   |                          |             |             |                      |                       |     |
     |   Queensland |   4654     29734         |  3445  79.2 |     0   0.0 |63.6  4.5  19.6  20.1 |87.3  39.2  48.5  72.4 | 0.0 |
     |   NSW        |  71790    361298         | 43562  64.2 |     0   0.0 |67.3  2.6  20.6  20.8 |85.1  37.4  50.1  69.4 | 0.0 |
     |   Victoria   |  78675    452348         | 45796  57.2 |     3   0.0 |66.9  2.0  21.9  21.5 |88.9  35.8  50.8  71.9 | 7.7 |
     |   Tasmania   |   4565     25167         |  2974  61.8 |     0   0.0 |71.1  0.9  20.7  21.5 |86.9  37.7  44.1  71.8 | 0.0 |
     |   SA         |  24867    144349         | 16239  69.0 |     0   0.0 |62.7  3.0  20.6  21.3 |91.3  34.3  51.1  72.5 | 0.0 |
     |   WA         |  34167    235755         | 24560  76.1 |     0   0.0 |63.5  1.7  19.1  21.0 |87.8  29.7  49.2  68.6 | 0.0 |
     |--------------|--------------------------|-------------|-------------|----------------------|-----------------------|-----|
     |   Australia  | 218718   1248651         |136576  64.8 |     3   0.0 |65.9  2.3  20.8  21.2 |87.8  34.9  50.1  70.6 | 7.7 |
     |--------------|--------------------------|-------------|-------------|----------------------|-----------------------|-----|
     | TYPE:        |                          |             |             |                      |                       |     |
     |   Fleece     | 127676    815955         |103160  78.8 |     3   0.0 |69.6  1.4  21.1  20.4 |90.5  36.2  50.7  73.8 | 7.7 |
     |   Skirting   |  51674    242255         | 28295  57.0 |     0   0.0 |56.3  5.0  19.5  21.8 |80.7  29.7  53.3  60.5 | 0.0 |
     |   Carding    |  39368    190441         |  5121  14.6 |     0   0.0 |62.0  2.8  21.1  23.7 |60.3  29.2  21.2  43.7 | 0.0 |
     |==============|==========================|=============|=============|======================|=======================|=====|
     | 2024/2025:   |                          |             |             |                      |                       |     |
     |   Queensland |   2825     17426         |  2142  82.1 |     0   0.0 |63.4  3.4  19.1  20.2 |89.0  35.8  48.0  72.7 | 0.0 |
     |   NSW        |  66101    341239         | 40168  65.0 |     0   0.0 |66.7  2.6  20.5  20.8 |87.5  36.3  45.3  71.1 | 0.0 |
     |   Victoria   |  75140    458234         | 45026  59.3 |     0   0.0 |65.1  2.0  21.4  21.9 |89.5  34.5  46.1  72.2 | 0.0 |
     |   Tasmania   |   5373     29656         |  3676  65.0 |     0   0.0 |70.5  0.7  20.2  21.5 |89.2  35.9  42.1  72.4 | 0.0 |
     |   SA         |  14819     84839         |  9524  67.4 |     0   0.0 |60.7  2.9  20.4  21.8 |89.8  32.8  45.3  71.5 | 0.0 |
     |   WA         |  28858    191583         | 21100  77.2 |     0   0.0 |62.9  1.7  18.8  21.4 |86.6  28.0  48.5  67.0 | 0.0 |
     |--------------|--------------------------|-------------|-------------|----------------------|-----------------------|-----|
     |   Australia  | 193116   1122977         |121636  65.2 |     0   0.0 |65.0  2.2  20.5  21.4 |88.3  33.7  46.2  70.8 | 0.0 |
     |--------------|--------------------------|-------------|-------------|----------------------|-----------------------|-----|
     | TYPE:        |                          |             |             |                      |                       |     |
     |   Fleece     | 114099    740936         | 92513  79.0 |     0   0.0 |68.5  1.4  20.7  20.7 |90.9  34.9  46.4  74.0 | 0.0 |
     |   Skirting   |  44904    214868         | 24806  57.5 |     0   0.0 |55.2  4.9  19.2  21.9 |80.8  29.2  50.7  60.9 | 0.0 |
     |   Carding    |  34113    167173         |  4317  13.8 |     0   0.0 |61.6  2.6  21.2  24.1 |59.7  26.3  18.1  41.3 | 0.0 |
     |==============|==========================|=============|=============|======================|=======================|=====|
     | DIFFERENCES: |                          |             |             |                      |                       |     |
     |   Queensland |  39.3-     41.4-   40.9- |  37.8-  2.9 |   0.0   0.0 | 0.2- 1.1-  0.5-  0.1 | 1.7  3.4-   0.5-  0.3 | 0.0 |
     |   NSW        |   7.9-      5.6-    5.0- |   7.8-  0.8 |   0.0   0.0 | 0.6- 0.0   0.1-  0.0 | 2.4  1.1-   4.8-  1.7 | 0.0 |
     |   Victoria   |   4.5-      1.3     1.5  |   1.7-  2.1 | 100.0-  0.0 | 1.8- 0.0   0.5-  0.4 | 0.6  1.3-   4.7-  0.3 | 7.7-|
     |   Tasmania   |  17.7      17.8    17.8  |  23.6   3.2 |   0.0   0.0 | 0.6- 0.2-  0.5-  0.0 | 2.3  1.8-   2.0-  0.6 | 0.0 |
     |   SA         |  40.4-     41.2-   41.4- |  41.4-  1.6-|   0.0   0.0 | 2.0- 0.1-  0.2-  0.5 | 1.5- 1.5-   5.8-  1.0-| 0.0 |
     |   WA         |  15.5-     18.7-   18.6- |  14.1-  1.1 |   0.0   0.0 | 0.6- 0.0   0.3-  0.4 | 1.2- 1.7-   0.7-  1.6-| 0.0 |
     |--------------|--------------------------|-------------|-------------|----------------------|-----------------------|-----|
     |   Australia  |  11.7-     10.1-    9.9- |  10.9-  0.4 | 100.0-  0.0 | 0.9- 0.1-  0.3-  0.2 | 0.5  1.2-   3.9-  0.2 | 7.7-|
     |--------------|--------------------------|-------------|-------------|----------------------|-----------------------|-----|
     |   Fleece     |  10.6-      9.2-    9.0- |  10.3-  0.2 | 100.0-  0.0 | 1.1- 0.0   0.4-  0.3 | 0.4  1.3-   4.3-  0.2 | 7.7-|
     |   Skirting   |  13.1-     11.3-   11.0- |  12.3-  0.5 |   0.0   0.0 | 1.1- 0.1-  0.3-  0.1 | 0.1  0.5-   2.6-  0.4 | 0.0 |
     |   Carding    |  13.3-     12.2-   12.6- |  15.7-  0.8-|   0.0   0.0 | 0.4- 0.2-  0.1   0.4 | 0.6- 2.9-   3.1-  2.4-| 0.0 |
     |______________|__________________________|_____________|_____________|______________________|_______________________|_____|

     NOTE: AR% = Adoption Rate %, i.e. % of number of bales tested for Staple Measurement and Colour (Average Yellowness).
           Differences in LOTS, BALES, and WEIGHT are year-on-year % differences.
           Differences in ADOPTION RATE % and in the TEST RESULTS are year-on-year actual differences.
           Change in SUPERFINE production (ktonnes) = -3.9%.
           It has moved from 53.8% of the clip at the end of FEBRUARY  last year to 57.3% this year.
           Hauteur is calculated using the TEAM-3 formulae as of July 1st, 2006.

                                       SUPERFINE PRODUCTION - JULY TO FEBRUARY,  2024/2025                                       Page  6
      _________________________________________________________________________________________________________________________________
     |              |                                                                 |                                                |
     |              |                        WEIGHT (tonnes)                          |            PERCENTAGE OF TOTAL CLIP            |
     |              | 0.0-16.5  16.6-17.5  17.6-18.5  18.6-19.5 |  0.0-19.5 | ALL WOOL| 0.0-16.5 16.6-17.5 17.6-18.5 18.6-19.5|0.0-19.5|
     |______________|___________________________________________|___________|_________|_______________________________________|________|
     | 2023/2024:   |                                           |           |         |                                       |        |
     |   Queensland |   221.4      476.0      798.0     1453.9  |   2949.4  |         |    4.1       8.8      14.7      26.8  |  54.4  |
     |   NSW        |  5795.3     9373.5    11936.3    10597.6  |  37702.7  |         |    9.1      14.7      18.7      16.6  |  59.0  |
     |   Victoria   |  3305.0     7178.6    12583.7    13324.3  |  36391.6  |         |    4.1       8.9      15.6      16.5  |  45.0  |
     |   Tasmania   |   759.7      983.3      868.4      365.9  |   2977.2  |         |   17.0      22.0      19.5       8.2  |  66.8  |
     |   SA         |   206.1     1274.5     3698.6     5753.8  |  10933.0  |         |    0.8       4.9      14.2      22.1  |  41.9  |
     |   WA         |  1190.2     4704.2    10586.5    12312.5  |  28793.3  |         |    2.8      11.2      25.2      29.3  |  68.6  |
     |--------------|-------------------------------------------|-----------|---------|---------------------------------------|--------|
     |   Australia  | 11477.8    23990.0    40471.5    43808.0  | 119747.3  |         |    5.2      10.8      18.2      19.7  |  53.8  |
     |--------------|-------------------------------------------|-----------|---------|---------------------------------------|--------|
     | TYPE:        |                                           |           |         |                                       |        |
     |   Fleece     |  6898.9    13242.2    23031.9    28731.7  |  71904.7  |         |    4.7       9.0      15.7      19.6  |  49.0  |
     |   Skirting   |  3150.4     6514.1    10755.8    10408.8  |  30829.0  |         |    7.4      15.3      25.2      24.4  |  72.4  |
     |   Carding    |  1428.5     4233.7     6683.9     4667.5  |  17013.6  |         |    4.3      12.7      20.1      14.0  |  51.2  |
     |==============|===========================================|===========|=========|=======================================|========|
     | 2024/2025:   |                                           |           |         |                                       |        |
     |   Queensland |   100.6      204.7      775.2     1168.0  |   2248.5  |         |    3.1       6.4      24.2      36.5  |  70.2  |
     |   NSW        |  6216.9     8468.1    11136.4     9984.3  |  35805.7  |         |   10.2      13.9      18.3      16.4  |  59.0  |
     |   Victoria   |  4520.1     7981.8    12650.6    14056.3  |  39208.7  |         |    5.5       9.7      15.4      17.1  |  47.8  |
     |   Tasmania   |  1309.3     1147.4      836.3      335.9  |   3629.0  |         |   24.9      21.8      15.9       6.4  |  69.1  |
     |   SA         |   439.1     1171.6     2543.8     3484.3  |   7638.9  |         |    2.9       7.7      16.6      22.8  |  50.0  |
     |   WA         |  1812.0     5302.1    10304.0     9094.2  |  26512.3  |         |    5.3      15.5      30.1      26.6  |  77.6  |
     |--------------|-------------------------------------------|-----------|---------|---------------------------------------|--------|
     |   Australia  | 14398.0    24275.8    38246.3    38123.1  | 115043.2  |         |    7.2      12.1      19.1      19.0  |  57.3  |
     |--------------|-------------------------------------------|-----------|---------|---------------------------------------|--------|
     | TYPE:        |                                           |           |         |                                       |        |
     |   Fleece     |  8798.6    13869.3    23071.6    26404.0  |  72143.5  |         |    6.6      10.4      17.3      19.8  |  54.0  |
     |   Skirting   |  3937.7     6475.0     9918.7     8339.4  |  28670.7  |         |   10.4      17.1      26.1      22.0  |  75.6  |
     |   Carding    |  1661.7     3931.5     5256.0     3379.8  |  14229.0  |         |    5.7      13.5      18.1      11.6  |  49.0  |
     |==============|===========================================|===========|=========|=======================================|========|
     | DIFFERENCES: |                                           |           |         |                                       |        |
     |   Queensland |    54.6-      57.0-       2.9-      19.7- |     23.8- |    40.9-|    1.0-      2.4-      9.5       9.7  |  15.8  |
     |   NSW        |     7.3        9.7-       6.7-       5.8- |      5.0- |     5.0-|    1.1       0.8-      0.4-      0.2- |   0.0  |
     |   Victoria   |    36.8       11.2        0.5        5.5  |      7.7  |     1.5 |    1.4       0.8       0.2-      0.6  |   2.8  |
     |   Tasmania   |    72.3       16.7        3.7-       8.2- |     21.9  |    17.8 |    7.9       0.2-      3.6-      1.8- |   2.3  |
     |   SA         |   113.1        8.1-      31.2-      39.4- |     30.1- |    41.4-|    2.1       2.8       2.4       0.7  |   8.1  |
     |   WA         |    52.2       12.7        2.7-      26.1- |      7.9- |    18.6-|    2.5       4.3       4.9       2.7- |   9.0  |
     |--------------|-------------------------------------------|-----------|---------|---------------------------------------|--------|
     |   Australia  |    25.4        1.2        5.5-      13.0- |      3.9- |     9.9-|    2.0       1.3       0.9       0.7- |   3.5  |
     |--------------|-------------------------------------------|-----------|---------|---------------------------------------|--------|
     |   Fleece     |    27.5        4.7        0.2        8.1- |      0.3  |     9.0-|    1.9       1.4       1.6       0.2  |   5.0  |
     |   Skirting   |    25.0        0.6-       7.8-      19.9- |      7.0- |    11.0-|    3.0       1.8       0.9       2.4- |   3.2  |
     |   Carding    |    16.3        7.1-      21.4-      27.6- |     16.4- |    12.6-|    1.4       0.8       2.0-      2.4- |   2.2- |
     |______________|___________________________________________|___________|_________|_______________________________________|________|

                                       ULTRAFINE PRODUCTION - JULY TO FEBRUARY,  2024/2025                                       Page  7
      _________________________________________________________________________________________________________________________________
     |              |                                                                 |                                                |
     |              |                        WEIGHT (tonnes)                          |            PERCENTAGE OF TOTAL CLIP            |
     |              | 0.0-12.5  12.6-13.5  13.6-14.5  14.6-15.5  15.6-16.5  |ALL WOOL |0.0-12.5 12.6-13.5 13.6-14.5 14.6-15.5 15.6-16.5|
     |______________|_______________________________________________________|_________|________________________________________________|
     | 2023/2024:   |                                                       |         |                                                |
     |   Queensland |     0.0        0.0        1.1       20.9      199.5   |         |    0.0       0.0       0.0       0.4      3.7  |
     |   NSW        |    31.7       49.9      194.8     1188.0     4330.9   |         |    0.0       0.1       0.3       1.9      6.8  |
     |   Victoria   |     1.7       17.2       99.4      588.8     2597.9   |         |    0.0       0.0       0.1       0.7      3.2  |
     |   Tasmania   |     0.0        0.9        8.5      159.0      591.2   |         |    0.0       0.0       0.2       3.6     13.3  |
     |   SA         |     0.0        0.0        0.3        9.5      196.3   |         |    0.0       0.0       0.0       0.0      0.8  |
     |   WA         |     0.0        2.3       10.6      139.2     1038.2   |         |    0.0       0.0       0.0       0.3      2.5  |
     |--------------|-------------------------------------------------------|---------|------------------------------------------------|
     |   Australia  |    33.5       70.3      314.7     2105.3     8954.0   |         |    0.0       0.0       0.1       0.9      4.0  |
     |--------------|-------------------------------------------------------|---------|------------------------------------------------|
     | TYPE:        |                                                       |         |                                                |
     |   Fleece     |    25.1       45.3      202.6     1323.3     5302.6   |         |    0.0       0.0       0.1       0.9      3.6  |
     |   Skirting   |     7.3       22.1       96.0      585.2     2439.8   |         |    0.0       0.1       0.2       1.4      5.7  |
     |   Carding    |     1.0        2.9       16.1      196.9     1211.6   |         |    0.0       0.0       0.0       0.6      3.6  |
     |==============|=======================================================|=========|================================================|
     | 2024/2025:   |                                                       |         |                                                |
     |   Queensland |     0.0        0.0        0.5       18.9       81.2   |         |    0.0       0.0       0.0       0.6      2.5  |
     |   NSW        |    43.3       42.3      231.1     1331.5     4568.8   |         |    0.1       0.1       0.4       2.2      7.5  |
     |   Victoria   |     3.4       21.0      158.1      856.6     3481.0   |         |    0.0       0.0       0.2       1.0      4.2  |
     |   Tasmania   |     0.0        0.9       70.9      374.3      863.2   |         |    0.0       0.0       1.4       7.1     16.4  |
     |   SA         |     0.0        0.0        5.9       57.9      375.3   |         |    0.0       0.0       0.0       0.4      2.5  |
     |   WA         |     1.2       10.1       39.9      304.8     1455.9   |         |    0.0       0.0       0.1       0.9      4.3  |
     |--------------|-------------------------------------------------------|---------|------------------------------------------------|
     |   Australia  |    47.9       74.3      506.4     2944.0    10825.2   |         |    0.0       0.0       0.3       1.5      5.4  |
     |--------------|-------------------------------------------------------|---------|------------------------------------------------|
     | TYPE:        |                                                       |         |                                                |
     |   Fleece     |    33.1       47.0      340.7     1864.7     6513.0   |         |    0.0       0.0       0.3       1.4      4.9  |
     |   Skirting   |    13.6       22.1      131.8      850.6     2919.6   |         |    0.0       0.1       0.3       2.2      7.7  |
     |   Carding    |     1.2        5.2       33.9      228.8     1392.6   |         |    0.0       0.0       0.1       0.8      4.8  |
     |==============|=======================================================|=========|================================================|
     | DIFFERENCES: |                                                       |         |                                                |
     |   Queensland |     0.0        0.0       54.5-       9.6-      59.3-  |    40.9-|    0.0       0.0       0.0       0.2      1.2- |
     |   NSW        |    36.6       15.2-      18.6       12.1        5.5   |     5.0-|    0.1       0.0       0.1       0.3      0.7  |
     |   Victoria   |   100.0       22.1       59.1       45.5       34.0   |     1.5 |    0.0       0.0       0.1       0.3      1.0  |
     |   Tasmania   |     0.0        0.0      734.1      135.4       46.0   |    17.8 |    0.0       0.0       1.2       3.5      3.1  |
     |   SA         |     0.0        0.0     1866.7      509.5       91.2   |    41.4-|    0.0       0.0       0.0       0.4      1.7  |
     |   WA         |     0.0      339.1      276.4      119.0       40.2   |    18.6-|    0.0       0.0       0.1       0.6      1.8  |
     |--------------|-------------------------------------------------------|---------|------------------------------------------------|
     |   Australia  |    43.0        5.7       60.9       39.8       20.9   |     9.9-|    0.0       0.0       0.2       0.6      1.4  |
     |--------------|-------------------------------------------------------|---------|------------------------------------------------|
     |   Fleece     |    31.9        3.8       68.2       40.9       22.8   |     9.0-|    0.0       0.0       0.2       0.5      1.3  |
     |   Skirting   |    86.3        0.0       37.3       45.4       19.7   |    11.0-|    0.0       0.0       0.1       0.8      2.0  |
     |   Carding    |    20.0       79.3      110.6       16.2       14.9   |    12.6-|    0.0       0.0       0.1       0.2      1.2  |
     |______________|_______________________________________________________|_________|________________________________________________|